### ASPHALT PAVEMENT REPAIR

## Summary of Work

Remove and replace asphalt paving and base in specific areas as specified by the Project Manager.

Apply soil sterilant in all areas where repairs are to be made at the

manufacturer’s prescribed rate of application.

- Arsenal

- Roundup

Asphaltic Concrete mix requirements:

- Asphalt Cement

- Meet requirements of ASTM D 3381, Viscosity grade as follows-

- AC5 in Cold Climatic Conditions

- AC10 in Moderate Climatic Conditions

- AC20 in Hot Climatic Conditions

- Aggregates

Fine to course mineral aggregates with wear less than 40 percent as determined by ASTM 131 and mineral filler suitable for pavement with a ¾” maximum aggregate size for full depth patches and 3/8” maximum aggregate for skin patches.

Repair of deteriorated areas.

- Cut edges of pavement in a rectangular shape and for 12 inches minimum beyond the damaged material.  All vertical cuts shall be made using a pavement saw.  All debris shall be removed to a legal dumpsite daily or to a stockpile location approved by the Project Manager so that the material can be removed at the end of the project.

- Base course – install a leveling course of crusher run gravel:

- Four inches thick after compaction.

- Mechanically compact to Ninety-five percent minimum density as determined by ASTM D 1557.

- Finish base course shall be true to line and grade within plus or minus ¼ inch in ten feet.

- Apply emulsion tack coat to vertical edges of existing asphalt and curbs.

- Paving –

- Place full depth at temperatures between 250 and 325 degrees F.

- Compaction –

- Compact asphaltic concrete paving to 92 percent minimum of design density as determined by ASTM D1559

- Roll with powered equipment capable of obtaining specified density.  Vibrator plate compactor may be used for areas too small to use larger equipment.

- Begin breakdown rolling immediately after asphalt is placed when temperature is at it’s maximum.  Complete rolling when temperature drops below 240 degrees F.

- Start intermediate rolling as soon as possible after breakdown rolling is complete and before mix temperature drops below 185 degree F.

- Execute compaction so visibility of joints is minimized.  Complete finish rolling to improve asphalt surface as soon as possible after intermediate rolling and while asphalt is still warm.  Do not use vibration for finish rolling.

- Skin patching.

- Area to be cleaned from debris will be prepared thoroughly by the means of blowing, sweeping and washing.

- Apply a bituminous tack coat to all surfaces.

- Patches not to exceed one inch of thickness

- Only 3/8” type “D” asphalt to be used and rolled with a Vibrator plate compactor.

- Surface shall be uniform with no birdbaths.  Leave surfaces clean and smooth.  Variations from specified grades shall not exceed ¼” in ten feet and have positive drainage.

CLEANING

Upon completion of repair operations, clean up and remove debris.