Scope of Work

# Concrete Balcony replacement

Demolition

- Remove the existing concrete topping and waterproofing membrane.  Replace all damaged framing material as required.

- Remove the stucco around the perimeter of the sliding glass door approximately 12” away from the opening and around the perimeter of the deck at the building and all guardrail walls to a height of approximately 12”

- Remove the existing sliding glass door and save for reuse.

- Remove the existing metal rails and save for reuse.

Preparation

- Install ¾” Tongue and Groove exterior grade plywood with all edges supported in the field of the balcony deck.

- Install a 1 ½” x 3’ metal L – flashing turned down over the edges of all plywood at the open perimeter of the deck.

Balcony Waterproofing

- Install a continuous sheet waterproofing system as manufactured by W. R. Grace Inc., Bituthene P-3000 Membrane and Bituthene Liquid Membrane materials.

- Lap the membrane up the walls a minimum of 8” and into the sliding glass door opening and seal all laps with Bituthene Mastic.

- Lap the sheet waterproofing system over the turned down flashing at the open perimeter of the balcony deck.

- Install new L- metal flashing with solid preformed corners around the perimeter of the deck, integrating into the stucco lath and building felt, shingle fashion.

- Install a pre-formed sill pan flashing in the opening for the sliding glass door lapping over the L-metal flashing that runs along the full perimeter of the deck.  The horizontal leg of the sill pan shall not be penetrated with fasteners.

- The joints of all flashing shall either be soldered or sealed with mastic on both the horizontal and vertical legs.

Concrete topping

- Install a preformed aluminum T bar concrete pour stop per the details.  The pour stop shall be supported on bituthene washers spaced 12” on center to create a weep hole.  Secure the  T bar with stainless steel self tapping screws at 24” on center.

- Install a 3000 psi (at age 28 days)  hardrock concrete topping slab with Fibermesh reinforcement at a minimum thickness of 2”.

- Moist cure the slab and protect from damage until fully cured.

Finishes

- Reinstall the sliding glass door after wrapping the opening with a 6” wide layer of self sealing bituthene in a shingle fashion.

- The existing stucco shall be carefully scabbed off of the existing lath a minimum of 6” to allow for integration of new lath and building paper at all areas where the stucco was removed.

- Install solid zinc – preformed stucco accessories to match existing or as required for a proper finish.  The lower edge of all stucco shall terminate with a weep screed.

- Provide a 3 coat, 7/8” thick Portland cement based stucco system over expanded diamond mesh, self-furring HDG lath.  The building paper shall be a 15# asphalt saturated felt, lapped shingle fashion and integrated into the existing.  Seal all butt joints in felt with Sonneborn HLM-5000 liquid waterproofing membrane.

- Provide an acrylic based textured finish coat to match the existing texture and color.

- Reinstall the metal guardrails setting all fasteners in urethane sealant.