## Pool replastering with white marble plaster

The Contractor shall complete all the work specified herein in a professional and workman-like manor according to the highest standards of the trades. All work shall comply with all applicable federal (OSHA\ state and local requirements. All work shall comply with the building and fire codes of the local jurisdiction. All building materials shall be new and shall be applied according to the manufacturers' specifications and/or recommendations unless specified otherwise. The scope of work shall include all items as specified by the Project Manager and indicated in the bid proposal.

  - Submit mix design of plaster prior to application.

  - Submit tile colors, markers, etc. as applicable per the scope of work for approval by the Project Manager.

The following materials shall be used unless the Project Manager specifically approves substitutions or alternates

- Pool Surface

  - Portland Cement:  ASTM C150 Type 1, white

  - Fine Aggregate: Crushed Marble, pool mix, white

  - Water: Potable only

  - Admixture: Berylex ® or equal

  - Bonding Agent: Bond Kote ® manufactured by SGM Inc., 800-641-9247

- Deck

  - Portland Cement: ASTM C150 Type 1

  - Fine Aggregate: ASTM C33, natural sand

  - Coarse Aggregate: ASTM C33, gravel or stone, maximum ¾”, standard weight

  - Water: Potable only

  - Reinforcing:  #4 R. B. at 16” o.c. for all new work.

  - Air Entraining Agent: submit for approval.

  - Granular Cushion:  4” layer of ¾” stone or gravel.

  - Pre-mold Expansion Joint: ½” by depth of concrete with Zip Strip.

  - Sealant: Vulkem or Dec-O-Seal

Installation of plaster:

- Pool Surface

  - Preparation:

- Secure, if necessary, any permits to perform the contracted work.

- Turn off or disconnect any and all equipment.

- Drain water from pool in accordance with local city codes and where necessary remove hydrostatic plug or drill holes in bottom of pool to prevent uplift.

- If applicable, remove tiles.

- Undercut all tile rows, drains, skimmers and other surface penetrations to original substrate as necessary.

- Prepare surface by chipping out old plaster down to gunite.

- Treat all exposed rebar with rust inhibitor and brown coat as required.  First four (4) treatments per pool or spa are included.  Any additional, after Project Manager’s visual verification, will be change ordered at no more then $25. Each.

  - Placing new plaster surface:

- Install new tiles or repair existing as specified by the Project Manager.

- Set depth markers and tiles at all benches, steps and/or any changes in elevation required by code.  Depth markers are to be visible above waterline.

- Apply bonding agent per manufacturer’s requirements.

- White marble plaster is to be applied in two (2) coats.  Each coating in a uniform layer 1/4” to 1/2” thickness with all exposed edges rounded off and a smooth, tight surface throughout.

- The placement of the plaster shall be coordinated in such a manner as to assure that a continuous pour occurs and that the plaster has no joints of any kind.

C.   Completion:

- Install new hydrostatic plugs as necessary.

- Fill pool immediately.  Filter all non-potable water to remove any suspended particles to prevent any staining, discoloration or damage to the new surface during the filling process.

- Provide written maintenance procedures at completion to include chemical balancing and treatments.

- Start up to include all necessary chemicals to treat water and to assure proper curing of new plaster.

- Contractor is responsible for keeping construction area clean and free of debris at the end of each workday.

- Contractor is to remove all debris to a safe and legal offsite dump as part of this contract.

- Deck repairs or replacements (If Specified)

  - Placing new concrete.

- Remove concrete to be repaired or replaced.

- Mechanically compact all soils prior to placement of new concrete.

- Place 4” thick, 3500 psi (at age 28 days) concrete with 5% air entrainment.

- Place #4 reinforcing bars at 16” on center each way in center of concrete.

- Place all new reinforcing on plastic chairs.

- Place all new concrete in a uniform manner, consolidating around reinforcement and all penetrations.

- Provide ½” diameter by 18” long smooth dowels embedded 9” into existing concrete at 32” on center at the perimeter of all new concrete sections.

- Moisture cure for a minimum of 48 hours.  Do not apply any curing agents to new concrete surface.

- Install new Kook Deck plaster coating as specified by the Project Manager, color as selected by the Project Manager.

  - Deck resurfacing

- Sound deck for voids, remove loose and spalling deck materials.

- Power wash deck with a 3000-psi or stronger power washer to remove all dirt and oil.

- Chase cracks with a 4” grinder and fill with 5000-psi epoxy.

- Add two (2) feet of bubble pack around perimeter of pool to prevent material from falling into pool.

- Float deck completely with acrylic epoxy polymer cement equal to or better then Ver-Crete VC700 decorative concrete system manufactured by Veron Coating Systems, Phoenix, AZ.

- Apply texture coat, prep, and stain with two (2) coats of acrylic urethane color coat equal to or better then Veron Coating System VC135p manufactured by Veron Coating Systems, Phoenix, AZ.

- Add a series of saw cuts if needed for future deck movement.