# Asphalt sealcoating using “Star” Sealcoat products

Scope of Work  	Includes Sealing in conformance with this specification.

1.	Crackfilling of all cracks larger than ¼” in width.

2.	Spot priming all oil spots.

3.	Striping parking lot per Owner’s requirements.

Provide a sealer consisting of the following products and having a consistency suitable for troweling, squeegee, brush or spray application after thorough stirring and containing no clay or other deleterious substance.

a.   Sealcoat: Star Seal Coal tar pitch emulsion

b.   Additive: Star Macro-flex

c.   Crack fillers: Star Sta-flex or Sta-flex Supreme

d.   Primer: Star S.O.S. or Star One Step

e.   Striping Paint: Star Brite Plus fast drying 100% acrylic paint.

- Water shall be clean and potable, free of harmful soluble salts and

within a temperature range of 50 to 80 degrees.

APPLICATION OF SEAL COAT

1.	Prepare all surfaces  and clean all debris and chemicals from the

surfaces.  Embedded dirt and silt shall be removed with a steel bristle

hand broom and oil free compressed air blowers.

              - Clean all soil or vegetation from cracks in the paving.

              - Fill all cracks larger than ¼” with a cold pour crack filler.

2.	Prior to application of the sealcoat, all deposits of grease or oil shall be

cleaned by scraping, burning or cleaned with a detergent to remove all

residue.  The area shall be primed with an oilseal after preparation.

3.	The oilseal shall be a quick drying emulsion with suitable

admixtures to allow for isolating the sealcoat from any residues of oils or

oil deposits and compatible with the sealcoat material.

4.	The Star Seal product shall be applied according to the

manufacturer’s  recommended Moderate Traffic system as shown

in Table II under section 4.0 Materials and Recommendations from

their standard specicications.  A copy of these can be obtained

from the manufacturer or the Project Manager.

5.          The Contractor must submit the delivery tickets indicating the

quantity of product purchased and used for each project with their

invoice prior to the Owner making final payment.

6.	Apply the first coat of the  sealer by squeegee in parallel lines,

continuous over the area to be applied at a rate of 0.20 gallons per

square yard.  The second coat shall be spray applied perpendicular to the first coat after proper curing of the first coat.  The second coat shall be applied at a rate of 0.15 gallons per square yard.

7.	Achieve a finished surface seal which, when dry and thoroughly

set, is smooth, tough resilient, of uniform black color and

free from coarse textured areas, lap marks, ridges, and other

surface irregularities.

- Allow the sealcoat to cure a minimum of 24 hours prior to application of striping paint.  The Contractor shall review all striping plans with the Project Manager prior to commencement of this portion of the project.

PROTECTION  OF THE COMPLETED SEALCOAT AREA

1.	Protect the asphaltic concrete paved areas from traffic until the

sealer is set and cured and does not pick up under foot or

wheeled traffic.

2.    	Remove any sealer which has splashed onto adjacent surfaces or

repaint damaged curbs as required to return the surface to its original

condition.

3.	The contractor shall be responsible for coordinating the sealcoat job with

the onsite management and assuring that all  sprinkler systems are not

functioning on the day of the proposed work in the area to be sealed.