ASPHALT SHINGLE ROOFING SYSTEM

NOTE ** CertainTeed fiberglass and organic asphalt shingles.

NOTE **

NOTE ** This section is based on The CertainTeed Roofing Collection(TM), the country's most extensive line of fiberglass and organic asphalt shingles.  CertainTeed pioneered the concept of multi-layered shingles, widely known today as "architectural" shingles, and has led the industry in color innovation with complex color blending technology and the introduction of bold designer shingle colors such as variegated reds, blues and greens.

NOTE **

NOTE ** For more information on CertainTeed products and availability, or for the name of your local CertainTeed representative, call or write:

NOTE **     CertainTeed Architectural Support Group

NOTE **     P.O. Box 860

NOTE **     Valley Forge, PA 19482

NOTE **     Tel:  (800) 233-8990

NOTE **     Fax:  (610) 341-7940

This specification includes installation of the following:

1.	Granule surfaced asphalt shingle roofing.

2.	Moisture shedding underlayment, eave, valley and ridge protection.

3.	Associated metal flashing.

NOTE ** Delete the following paragraph unless unusual project conditions mandate shop drawings.

WARRANTY REQUIREMENTS

1.	NOTE ** Edit the following warranty requirements to conform to shingle types specified.

1.Manufacturer's Warranty.  Contractor shall furnish the shingle manufacturer's 30-year warranty for products of this section. During the warranty period, Contractor shall guaranty a response time to documented leaks or other failures within a 48-hour period.

2.	Warranty Supplement.  Contractor shall provide an installer’s supplemental warranty that covers labor in the event of problems or defects for a period of one year after completion of application of shingles.

3.	Warranty Transferability Clause.  Contractor shall make the shingle manufacturer’s standard option for transferring the warranty to a new owner available to Owner.

PRODUCTS

MANUFACTURER

1.	Provide products manufactured by GAF Corporation, 1361 Alps Road, Wayne, New Jersey 07470, telephone number 1-800-766-3411.

NOTE ** Delete shingle types not required for the building project.

2.	GAF/ELK 30yr Timberline Natural Shadow:  Conforming to ASTM D 3018 Type I - Self-Sealing; ASTM D 3161/UL997 Wind Resistance, and UL Class A Fire Resistance; glass fiber mat base, ceramically colored/UV resistant mineral surface granules across entire face of shingle, architectural type.

NOTE ** Retain one of the following two sub-paragraphs; first is for East Coast and Northeast Regions, second is for Lake Central and North Central Regions.

IIIIIaaNOTE ** Retain one of the following two sub-paragraphs, depending on color selection method.

333333Color:  As selected by the Owner from manufacturer's standard line of colors.

SHEET MATERIALS

NOTE ** Delete paragraph below and installation instructions in Part 3 if climatic conditions are such that ice dam protection is not required.

NOTE ** Select underlayment from the following three paragraphs, deleting those not required.  The CertainTeed "Roofers' Select" underlayment resists "hygro-expansion," significantly reducing wrinkling.

1.	Underlayment.  Underlayment shall be Tri Built AST or 15#, asphalt-impregnated fiberglass-reinforced organic felt designed for use on roof decks as a water-resistant layer beneath roofing shingles.

FLASHING MATERIALS

1.	Sheet Flashing.  Sheet flashing shall be non-corroding, non-staining 26-gage galvanized steel metal flashing or 0.027 aluminum flashing material.

ACCESSORIES

1.	Nails.  Use standard, round, wire-type roofing nails that are corrosion resistant; hot dipped, zinc-coated steel, aluminum or chromated steel, with a minimum of 3/8 inch (9.5 mm) head diameter; a minimum 11-gage (2.5 mm) shank diameter, and of sufficient length to penetrate through roof sheathing or 3/4 inch (19 mm) into solid wood, plywood or non-veneer wood decking.  Staples are not allowed on this job.

- Plastic Cement.  Use ASTM D 4586, asphalt roof cement.

- Venting.  Contractor shall use AF 50" Air Vents, installation per manufacturer’s requirement.

FLASHING FABRICATION

1.	Form flashing to existing roof profiles so roofing materials are protected from physical damage and shed water.

2.	Form sections square and accurate to existing roof profile, in maximum possible lengths and free from distortion or defects detrimental to appearance or performance.

ROOF DECK PREPARATION

- Broom clean deck surfaces under eave protection and underlayment before their application.

- New flashing shall be installed at all locations including, but not limited to, the following:

    - Eave drip edge flashing

    - Rake flashing

    - Step flashing at walls and chimneys

    - Counterflashing as required at cladding materials

    - No caulk flashings at roof penetrations, galvanized with rubber boot

    - Saddle flashing at any arbors or beams

    - Chimney caps

INSTALLATION - PROTECTIVE UNDERLAYMENT

NOTE ** Delete 2 paragraphs below if all roof slopes are greater than 4:12.  Otherwise, select either complete WinterGuard underlayment or D 4869 underlayment in combination with eave ice dam protection.  WinterGuard is an improved version of standard underlayment, developed to resist standing water held on a sloped roof at eaves and valleys by ice dams and to resist wind-driven water.  WinterGuard can be used to cover the entire roof deck, rather than just eaves and valleys, when the slope is so low (2-4:12) as to permit wind to drive rain beneath the shingle.

1.	Roof Slope Between 2:12 and 4:12:  Apply one layer of “Weather Watch” or “Storm Guard” over areas not already protected at eaves, with ends and edges weather lapped a minimum of 6 inches.  Stagger end laps each consecutive layer.  Nail in place.

2.	Roof Slope Between 2:12 and 4:12:  Apply two layers of D 4869 underlayment over areas not protected by “Weather Watch” or “Storm Guard” at eaves, with ends and edges weather lapped a minimum of 19 inches.  Stagger end laps each consecutive layer.  Nail in place.

3.	Roof Slope 4:12 or Greater:  Install one layer asphalt felt shingle underlayment perpendicular to slope of roof and lap minimum 4 inches over eave protection.

4.	Weather lap and seal watertight with plastic cement items projecting through or mounted on roof.  Do not allow solvent-based cements to contact “Weather Watch” or “Storm Guard”.

INSTALLATION - METAL FLASHING

1.	Weather lap joints minimum 2 inches (50 mm).

2.	Drip edges flashing along the rakes shall be placed on top of the underlayment.  Drip edge flashing along the eaves shall be placed under the underlayment.

INSTALLATION - ASPHALT SHINGLES

- Install shingles in accordance with manufacturer's instructions for product type and application specified.

- There shall be a minimum of 4 nails per shingle.  Shingles are to be installed per manufacturer’s specifications, below the tab seal line and above the cut out tab.  Florida and certain coastal areas have specific nailing requirements in addition to those noted in this specification.  It shall be the Contractor’s responsibility to determine local requirements for fastening of shingles.

- Before applying the first course of shingles, a row of asphalt shingles or a minimum 9-inch starter strip of mineral surfaced asphalt roll roofing material shall be applied along the edge of the eaves.

- Materials shall be fastened with a roofing nail along a line that is parallel to and 4 inches above the eaves edge.  The nail should be placed in such away that the nail heads will not be exposed to either cut outs or spaces between shingle tabs on the first course.

- The first course of shingles shall be started with full shingles, and succeeding courses should be started with full or cut shingles, depending upon the style of shingles being applied and the desired pattern.

- Asphalt shingles should be butted and nailed as they progress up either side of a hip or ridge.

- Cut back plywood 1.5" on each side of the ridge to allow for new ridge vent.

- Install 9" V-300 Cora Vent per manufacturers specifications at all ridge locations.

- Each end of the ridge vent shall be extended a minimum of 6” beyond the ventilation opening in the ridge.  A 2” opening shall be cut in deck at ridge.

- Ridge vents shall be installed with an aluminum bodied or mastic roof sealant at all vent-to-roof contact surfaces.

- Ridge vents shall be secured to roof using ring shank nails or screws.  Nails shall be no less than 2½” or penetrate decking 1-1/4” and spaced twelve inches (maximum) on center.

- Upper and lower vent overlay joints and all nail heads shall be sealed using a polyurethane caulk color to match shingles.

- Openings at each end of the ridge vent shall be closed using products supplied by the manufacturer.

FIELD QUALITY CONTROL

The Project Manager will provide a visual inspection of the Work. If any conditions are found to be unacceptable, the Contractor shall remove and reinstall that specific condition to meet the manufacturer’s installation specifications and recommendations.